# Text boxes

Vision Window:

170 x 110(mm)

The shield is designed and fabricated with higher standard than those required by governments or organization to better protection.

Arm Hanger:

For hanging on the arm purpose

Handle

For holding purpose

Radius of arc: 500mm

Width: 510mm

L:860mm

W:5.12kg

Shield Body:

It’s made of high intensity bulletproof cloth through thermal pressure process. The edge of the shield body is protected by heavy duty rubber.

- BS-1 is made of super strong bulletproof fiber cloth through high pressure curing process, the sturdy construction and high quality material give this ballistic shield an excellent bulletproof capability.

- Comply with American National institute of Justice Standard NIJ01018.01 Level IIIA standard.

- With ability to stop .44 SWC bullet, with 15.55g at 426m/sec speed.

- With ability to stop 9 mm FMJ Bullet, with 8g at 426m/sec speed

Supreme bulletproof capability

Raysun BS-1 Ballistic Shield